# WATER-BASED GLOSS CLEAR VINYL

**Temp Range: -40ºC - +80ºC**

**Min. Application Temp: +10ºC**

**Face:**

Clear, soft PVC film for short and medium term outdoor use.

**Thickness: 100 micron ±5%**

**Adhesive:**

Polyacrylate, permanent, transparent.

**Liner**

Silicone coated paper on one side.

**Basic Weight 135 gsm**