#  AUTOTEX F200 POLYESTER

**Face:**

High quality textured polyester film. For applications requiring a combination of high abrasion resistance and flexibility. Resistant to alcohols, dilute acids & alkalis, esters, hydrocarbons, ketone and household cleaning agents.

**Thickness: 200micron ±5%**

**Temp Range: -40ºC to +85ºC**

**Min. Application Temp: -40ºC**