# DIGITAL GLOSS CLEAR VINYL

**Temp Range: -30ºC - +110ºC**

**Min. Application Temp: +10ºC**

**Face:**

A high performance grade polymeric calendered self-adhesive vinyl . Suitable for application onto flat or slightly curved surfaces, such as vehicle graphics, retail signage and window graphics.

**Thickness: 70 micron ±5%**

**Adhesive:**

Permanent clear solvent-based acrylic.

**Initial Tack**:  **High**

**Final Adhesion: High**

**Liner**

Layflat kraft with PE coating.

**Thickness: 140 micron ±5%**